## Slide 1: Using Crushed Recycled Concrete Aggregate in Ready Mix
W. Scott Brown
Concrete Operations Manager, Anchorage Sand & Gravel

## Slide 2: Nomenclature:
Crushed Recycled Concrete Aggregate - RCA

## Slide 3: Inspiration To Batch RCA
Denver’s Stapleton Airport Demolition
  NRMCA Tour
  6.5 Million Tons Crushed Concrete
  Processed
  Ready Mix Plant on Site
  Performance Problems
    Strength Gain
    Severe Slump Loss
    Shrinkage

## Slide 4: Inspiration To Batch RCA
What to do with large stockpiles of crushed concrete?
How to make concrete industry more appealing to environmentally conscious project owners?
How to make Concrete industry more appealing to community?
How to make Concrete with RCA perform in structural applications?

## Slide 5: Early - R&D
Early Trial Batches
  W/C, Admix, Cement Content and Agg Blends
  Lots of sidewalk and patios
Same Problems
  Fine Aggregate Issues
  Strength Gain
  Slump Loss / Acceleration
  Shrinkage
  Garbage

## Slide 6: AS&G R&D
Mitigate the Usual Problems
  REMOVE THE FINES
Willing Aggregate Producer
  Cost Increase
Produced a ¾” X 3/8” Coarse Aggregate

## Slide 7: ¾” Coarse RCA
1” Minus Crushed Concrete
¾” 95.4%
½” 81.2%
3/8” 72.1%
#4 51.8%
#200 5.53%
¾” RCA
¾” 96.2%
½” 51.4%
3/8” 22.2%
#4 6.7%
#200 1.35%

## Slide 8: ¾” Coarse RCA
Physical Properties
LA Abrasion 27
Specific Gravity 2.497
Absorption 3.3
Dilution is the Solution
20% Coarse Replacement
  Maintain Slump
  Pumpability
  Strength
  Shrinkage

## Slide 9: ¾” Coarse RCA
100’s of yards placed in house.
  Footings
  SCC
  Exterior and Interior SOG

## Slide 10: Quality Control
Limiting Returned Concrete
Reduced Contaminates
Gradations
Tech Inspections

## Slide 11: Ave 28 Day Strengths – Mixes with 20% RCA
SCC 7200psi
.45 20% ASH AIR 5800psi
.45 20% ASH NON 7300psi
.50 ¾” MRWR AIR 5490psi
.45 ¾” 6” MRWR NON 8440psi

## Slide 12: Challenges
Maintaining Stockpile
Processing Costs
Agg Bin Space
Recycled Product
  Variability
Constant QC Monitoring
Its Different
  Guilty till proven innocent

## Slide 13: Market
Environmentally Concerned homeowners
Private Companies
Government projects looking to boost their recycled content

## Slide 14: University of Alaska Anchorage
Curb and Sidewalk
SCC – Walls

## Slide 15: Alaska Industrial Hardware - AIH
New Seward Hwy
Slab On Grades
Tailgated
Polished

## Slide 16: JBER – F-22 ADD/ALT Weapons Shop
USACE / Bristol Environment
Remodel and New Construction
Recycled Credits
20% Flyash
Footings
Slabs

## Slide 17: Towne Place Suites
Denny’s Construction
Marriot
Footings
Walls
Slabs
Shotcrete

## Slide 18: JBER – Buckner Fieldhouse
Bristol General Construction
Large Project
Footings
Walls
Interior / Exterior Slabs

## Slide 19: Other AS&G Products
Masonry Products
Waste Latex Paint
Which block contains Waste Latex Paint?

## Slide 20: Questions:
W. Scott Brown
Operations Manager
Anchorage Sand & Gravel
scott.brown@anchsand.com